## Slide 1: Transport, Continuity Equations and Simulation
Diffusion, Drift and FD

## Slide 2: Outline
Introduction to transport
  Diffusion
  Drift
  Continuity
Semiconductor transport equations
  Non-linearity
  Coupling
Complexity
Finite Difference Formulation
Examples
  Gaussian pulses
  PN diodes

## Slide 3: Definition of Particle Flux
 = particle flux, N = number of particles crossing A in a time interval t, A = area, t = time interval
Definition of Current Density
J = electric current density, Q = charge of the particle,  = particle flux
Particle flux/transport due to:
  Diffusion: Ficks first law, gradient drives flux, ~diffusivity
  Drift: Electric field drives flux (~E ~n) – we have used mobility to characterize this.
Sum both electrons and holes for complete flux
Einstein relations link mobility and diffusivity
Two mechanisms two carriers produce complex flows
Diffusion from high concentration to low
Steady-state no flow present
Presence of an impurity profile produces a built in field.
  In SS this implies an opposing field to balance the diffusion
Total Carrier Transport

## Slide 4
Drift of electrons in a conductor in the presence of an applied electric field. Electrons drift with an average velocity vdx in the x-direction. (Ex is the electric field.)
A current is a flow of charge through an area in a net amount of time.
We will often use current density J not I where:
I = J X Area.
Subtleties lie in vdx
Definition of current density

## Slide 5: Definition of Drift Velocity
vdx = drift velocity in x direction, N = number of conduction electrons, vxi = x direction velocity of ith electron
We define a drift velocity vd of an electron gas as the average velocity of all the electrons (usually in one direction – the direction of the applied electric field).
Generally we think of this drift as due to an applied E field

## Slide 6
Current Density and Drift Velocity
Jx (t) = envdx(t)
And we have both electrons and holes so:
This allows for a definition of the current density
vdx = dEx
Define a mobility μ where:
Drift Currents – Ohms law in point form

## Slide 7: Conductivity
 = conductivity, e = electronic charge, n = number of electrons per unit volume, d = drift velocity,  = mean scattering (collision) time = relaxation time, me = mass of an electron in free space.
If we know the number of electrons we can define a conductivity. Which gives J = σ E
We also use resistivity which is:

## Slide 8
(a) Arbitrary electron concentration n (x, t) profile in a semiconductor. There is a net diffusion
(flux) of electrons from higher to lower concentrations.
(b) Expanded view of two adjacent sections at x0. There are more electrons crossing x0 coming
From the left (x0-) than coming from the right (x0+)
Fick’s First Law
Electron Diffusion Current Density
Diffusion

## Slide 9
Arbitrary hole concentration p (x, t) profile in a semiconductor.
There is a net diffusion (flux) of holes from higher to lower concentrations. There are more
holes crossing x0 coming from the left (x0-) than coming from the right (x0+).
Hole Diffusion Current Density
JD, h = electric current density due to hole diffusion, e = electronic charge, h = hole flux, Dh = diffusion coefficient of holes, dp/dx = hole concentration gradient

## Slide 10: Derivation of Continuity Equation -- accounting equation (conservation of mass
Consider carrier-flux into/out-of an infinitesimal volume:
To solve for the time dependent n and p we need a differential equation that links flow to recombination and generation.
Full equation – derived a partial differential equation
  Divergence of the current flow must equal the net R/G
  Use simple life time for R/G from equilibrium value.

## Slide 11
Continuity
Equations:
With
And
Drift and diffusion

## Slide 12: Derivation of Minority Carrier Diffusion Equations
The minority carrier diffusion equations are derived from the general continuity equations, and are applicable only for minority carriers.
Simplifying assumptions:
  1. The electric field is small, such that
  in p-type material
  in n-type material
  2. n0 and p0 are independent of x (i.e. uniform doping)
  3. low-level injection conditions prevail

## Slide 13
Starting with the continuity equation for electrons ( and defining n = n0 + Δn where Δn is called the excess carriers and n0 is the equilibrium value:

## Slide 14: Carrier Concentration Notation
The subscript “n” or “p” is used to explicitly denote n-type or p-type material, e.g.
  pn is the hole (minority-carrier) concentration in n-type mat’l
  np is the electron (minority-carrier) concentration in n-type mat’l
Thus the minority carrier diffusion equations are

## Slide 15: Quasi-Fermi Levels
Whenever Dn = Dp  0, np  ni2. However, we would like to preserve and use the relations:
These equations imply np = ni2, however. The solution is to introduce two quasi-Fermi levels FN and FP such that

## Slide 16: Steady-State Continuity Equation for Holes
Continuity Equation with Uniform Photogeneration and no divergence of current
pn = pn - pno is the excess hole concentration
From Principles of Electronic Materials and Devices, Third Edition, S.O. Kasap (© McGraw-Hill, 2005)
Steady-State Continuity Equation with E = 0
Special Cases
Very often we can use simplified cases.

## Slide 17: Simplifications (Special Cases)
Steady state:
No diffusion current:
No R-G:
No light:
No E field:

## Slide 18
Non-uniform doping profile results in electron diffusion toward the less concentrated regions.
This exposes positively charged donors and sets up a built-in field Ex. In the steady state, the
diffusion of electrons toward the right is balanced by their drift toward the left.
Simple problem in the book solve for a 1D rod of material (open circuit configuration)
Assume N(x) = N0 e-x/b
Assume Steady-State
Set the total electron flow to zero
Complexity - Built in Field

## Slide 19
SS electron flow = 0
E is gradient of potential
Integrate the equation between limits gives built in field
Assume the N(x) is not disturbed significantly n2 and n1 are prescribed by doping. V2 and V1 are voltages at any points 1 and 2.
Use Einstein relation to simplify with
  E = grad V
  n ~ N(x)
Result is built in constant electric field
We can use this in the base of transistor to accelerate the electrons to the collector and increase the “speed” of the device.

## Slide 20
1D drift-diffusion equation
Two carriers and two transport mechanisms.
Life gets a bit complicated.
Total Electron Current Due to Drift and Diffusion
Total Hole Current Due to Drift and Diffusion
Einstein Relation
Photo-generation on Edge at Steady-State

## Slide 21
(a) Steady state excess carrier concentration profiles in
an n-type semiconductor that is continuously illuminated
at one end.
(b) Majority and minority carrier current components in
open circuit.
Total current is zero.
Diffusion equation for both carriers
Steady-state – flow of created electrons and holes at x=0 must be equal.
Generation at the edge – diffusion away with recombination occurring
Weak injection – majority carrier concentration is undisturbed
Different diffusivities/mobilities result in different distributions.
Two currents flow and tend to cancel out, but don’t quite.
As total current is zero there must be a drift current.
Drift current is due to majority carriers.
Minority carrier injection! -- is what we call this set of assumptions

## Slide 22
Assumption of diffusion only for minority carriers. Small field and few carriers mean insignificant drift current.
Presence of recombination gives a drop in the current (exp) as we move away from the surface.
Likewise, electrons also generated at surface diffuse away and we can solve the diffusion current for electrons.
Note this is only the current determined by diffusion – not the total electron current.
Derivation - Kasop
gives

## Slide 23: Electron Drift Current: Use the Open Circuit Condition
Now in steady-state the total current must be zero.
But the two diffusion currents are different due to Dh != De
And we can have a significant drift current for majority carriers (electrons) at a small field due large number of carriers.
So we can calculate the drift current that accommodates the difference in diffusion currents.
Drift is almost entirely majority carrier effect.
Difference in diffusion currents due to different effective masses and scattering.
Need to check that ρ = n – p that generates the E field is small and that low-level injection holds.
gives

## Slide 24: Numerical Modeling of drift-diffusion
Any real problem
  Transient
  Complex geometry or doping
  Is too difficult for analytical approaches
Numerical modeling is extensively used
  Coupled Potential, n and p equations or perhaps Efn and Efp
  Finite difference or FEM
  For good results need very fine mesh which makes simulation very slow
  Non-uniform meshing is essential due to non-linear nature of equations and doping profiles.
Example of 1D FD for SS and Transient.

## Slide 25
Numerical Approach
Numerical modeling of transport – finite difference
Solve Poisson’s Equation
Solve Transport Equations
Initial Guess for carrier density
No
Yes
Regardless how we start, all equations must be self-consistently satisfied at the same time
Converge! Or done
Notes: NEMO can provide the modeling essential for accelerating the development of nanoelectronics.
The physical model begins at the atomic level with the atomic orbitals. Efficient numerical algorithms allow NEMO to model practical semiconductor devices of several thousand atomic layers. NEMO includes the effect of open contacts, lattice vibration, alloy disorder and interface roughness to calculate macroscopic quantities such as the electron and hole density and the current.
The computational algorithms are accessed by a flexible graphical user interface (GUI) for rapid design prototyping and analysis. The figure at the right consists of screen dumps from the GUI chosen to illustrate its versatility.
The 3 figures in the upper right show
    the band profile of of an ultra-scaled MOS device with
    the electron charge calculated both semi-classically and quantum mechanically and
    the calculated and experimental tunnel current for different SiO2 barrier thicknesses.
  The two figures in the lower right display
    the band profile of an optoelectronic switch and
    the calculated quantum states of the device. The comparison of the experimental and calculated current for this device is shown in the lower right quadrant of the following slide.

## Slide 26
“Straight-forward” Method of Solving Transport Equations
In order to solve this equation, we first need to find a linear approximation to turn the differential equation into a discretized linear equation.
First step is to use the mesh point variables to interpolate the midpoint variables
Notes: NEMO can provide the modeling essential for accelerating the development of nanoelectronics.
The physical model begins at the atomic level with the atomic orbitals. Efficient numerical algorithms allow NEMO to model practical semiconductor devices of several thousand atomic layers. NEMO includes the effect of open contacts, lattice vibration, alloy disorder and interface roughness to calculate macroscopic quantities such as the electron and hole density and the current.
The computational algorithms are accessed by a flexible graphical user interface (GUI) for rapid design prototyping and analysis. The figure at the right consists of screen dumps from the GUI chosen to illustrate its versatility.
The 3 figures in the upper right show
    the band profile of of an ultra-scaled MOS device with
    the electron charge calculated both semi-classically and quantum mechanically and
    the calculated and experimental tunnel current for different SiO2 barrier thicknesses.
  The two figures in the lower right display
    the band profile of an optoelectronic switch and
    the calculated quantum states of the device. The comparison of the experimental and calculated current for this device is shown in the lower right quadrant of the following slide.

## Slide 27
“Straight-forward” Method of Solving Transport Equations
Solving the Transport Equations
Substitute the approximated variables back to transport equations
Continuity Equation tells us for steady-state (Gn = 0): Jn,i+1/2 = Jn,i-1/2
Ji-1/2
Ji+1/2
Continuity Equation tells us for Transient (Gn = 0):
nji = nij-1 + Δt div(Jn,ij-1 ) = nij-1 + Δt (Jn,i+1/2j-1 - Jn,i-1/2j-1 )/Δx
E = grad(V)
dn/dx
Notes: NEMO can provide the modeling essential for accelerating the development of nanoelectronics.
The physical model begins at the atomic level with the atomic orbitals. Efficient numerical algorithms allow NEMO to model practical semiconductor devices of several thousand atomic layers. NEMO includes the effect of open contacts, lattice vibration, alloy disorder and interface roughness to calculate macroscopic quantities such as the electron and hole density and the current.
The computational algorithms are accessed by a flexible graphical user interface (GUI) for rapid design prototyping and analysis. The figure at the right consists of screen dumps from the GUI chosen to illustrate its versatility.
The 3 figures in the upper right show
    the band profile of of an ultra-scaled MOS device with
    the electron charge calculated both semi-classically and quantum mechanically and
    the calculated and experimental tunnel current for different SiO2 barrier thicknesses.
  The two figures in the lower right display
    the band profile of an optoelectronic switch and
    the calculated quantum states of the device. The comparison of the experimental and calculated current for this device is shown in the lower right quadrant of the following slide.

## Slide 28: Code: Initial Setup
Choose Simulation run and run parameter file.
Create G matrix for Poisson eq. (V = G-1ρ) – use L, U formulation as it’s static.
Calculate μ and D
Initialize carrier densities from doping
Calculate net ρ from doping and carrier densities

## Slide 29: Code: Sim. Paras
Typical parameter file
Set simulation parameters
  Coupled (V and n, p are coupled)
  TwoCarriers – n and p or just n
  RC – recombination on/off
Set length and number of points
Add disturbance if wanted (Gaussian)
Set BC for V
Set stopping criteria
Set up plotting stuff

## Slide 30: Code: Poisson Eq
Set up G matrix for:
  V = G-1 ρ
Simple 1D finite difference
Bv vector used for boundary conditions
  Floating
  Fixed
Sparse for speed and memory

## Slide 31: Code: Main flow
Find initial V and E = dV/dx
  Courant-Friedrichs-Lewy time step criteria
  Get max Δt for diffusion:
    Δt < Δx2/Dn,p
  Get max Δt for drift:
    Δt < 2Δx/μE
Set up n and p
Two step simulation sometimes used – second simulation has new V BCs
SimulateFlow is the main loop

## Slide 32: Code: Main Loop
Loop to Tstop
Δt is set by CFL criteria (non-uniform time stepping)
Basic loop:
  First get V and E
  Next get divJn and divJp and update n and p
  Explicit for n and p
  Implicit for V
  If RC remove recombination Δn = Δp
  Recalculate ρ
  Back we go
Get V from rho
Reset dt if need
Get div(n) and update n
Get div(p) and update p
Calculate Recom. and update n and p
Add n and p to background doping to get rho

## Slide 33: Code: Jn divergence
Divergence of carriers uses J at halfway points
Use average μ and D
BC are either
  Zero flow (BC = 0)
  Fixed n or p at equilibrium (initial values) and divergence is zero.

## Slide 34: Single Carrier Gaussian packet
VbcL = VbcR = 0 so E ~ 0
Electrons diffuse out.
Jn = 0 at edges.
Final
Charge biases bulk negative
V = 0 at Edges cause a mirror image

## Slide 35: Single Carrier Gaussian packet
VbcL = 1 VbcR = 0.
Electrons diffuse out and drift left
Jn = 0 at edges.
Final
Charge accumulates on left side
Should self-limit when drift = diffusion

## Slide 36: Two Carriers Gaussian packet
VbcL = VbcR = 0 so E ~ 0
Electrons and holes diffuse out.
Dn != Dp so ρ is generated
No flow BC for carriers.
No net charge so no bias
Final
Holes and electrons diffuse together! Holes slow electrons down
Recombination eliminates non-equilibrium charge

## Slide 37: Two Carriers Gaussian packet
VbcL = 0 VbcR = 1
Electrons/holes diffuse out and drift to opposite sides
Jn = 0 at edges so accumulation
Final
No net charge
Very slow movement to equilibrium

## Slide 38: Exponential doping two carriers
VbcL = floating VbcR = 0
Self bias
Final
No net charge
Very slow movement to equilibrium

## Slide 39: Bookmark

## Slide 40
Example: PN Diode
The simplest semiconductor device is the PN diode.
We can view this as an initial diffusion of carriers both ways exposing ionized donors until large drift currents are established cancelling off the diffusion currents.
This requires a depleted region to form producing an electric field that creates the counter flowing drift current.

## Slide 41
(a) Two isolated p and n-type semiconductors (same material).
(b) A pn junction band diagram when the two semiconductors are in contact. The Fermi level
must be uniform in equilibrium. The metallurgical junction is at M. The region around M
contains the space charge layer (SCL). On the n-side of M, SCL has the exposed positively
charged donors whereas on the p-side it has the exposed negatively charged acceptors.
As with the Schotkky contact at equilibrium EF must be constant.
Built-in voltage Vo aligns the fermi energies.

## Slide 42
PN junction electrostatics – depletion approximation
The depletion approximation is analytical model assuming complete depletion of the interface region. This allows the electrostatics to be calculated for simple doping profiles.

## Slide 43
Energy band diagrams for a pn junction under
(a) open circuit and (b) forward bias. Note the displacement of the quasi-fermi levels.
Biasing the Diode: Forward bias lowers the barrier to carrier flow

## Slide 44
Forward biased pn junction and the injection of minority carriers.
Carrier concentration profiles across the device under forward bias.
The hole potential energy with and without an applied bias. W is the width of the SCL with forward bias.
np(0) is the electron concentration just outside the depletion region on the p-side
pn(0) is the hole concentration just outside the depletion region on the n-side
Forward biased pn junction and the injection of minority carriers.
If we assume low-level injection we can relate the carrier densities (under bias) at the depletion edges assuming thermionic excitation
“The Law of the Junction”

## Slide 45
The total current anywhere in the device is constant. Just outside the depletion region it is
due to the diffusion of minority carriers.
The injection of carriers across the depletion region will (forward bias) raise the minority carriers.
They will then diffuse across the neutral regions to the contacts forming hole and electron currents
These currents can be summed to find the total current as function of bias.
For long neutral regions the shape of the minority carrier distribution will be exponential due to recombination.
Away from the junction majority carrier drift current will carry part of the total current.

## Slide 46: Forward Bias: Diffusion Current
Hole diffusion current in n-side in the neutral region
There is a similar expression for the electron diffusion current density JD,elec in the p-region.
Ideal diode (Shockley) equation
Reverse saturation current
The total current is assumed to be the sum of the diffusion currents at the two edges of the depletion region.
Where it assumed that drift current is small.
This leads to the ideal diode equation.

## Slide 47
Minority carrier injection and diffusion in a short diode.
Short Diode
where ln and lp represent the lengths of the neutral n- and p-regions outside the depletion region.
The geometry of the diode changes the expression for J0
For a short neutral region recombination can be ignored and the distribution is linear.

## Slide 48
For a forward biased pn junction we have injection of excess carriers and their recombination in the SCL which produces a second current component.
Recombination Current
Total diode current = diffusion + recombination
The diode equation
Model ignores a number of effects.
Forward Bias

## Slide 49
Energy band diagrams for a pn junction under (c) reverse bias conditions; and
(d) thermal generation of electron hole pairs in the depletion region results in a small reverse current.
Reverse bias increases the barrier height and depletion width and we use the same analysis. However, we also get significant thermal generation in the depletion region as the carrier distributions are suppressed.

## Slide 50
Reverse biased pn junction. (a) Minority carrier profiles and the origin of the reverse current. (b) Hole PE across the junction under reverse bias
Reverse Bias
In reverse bias the thermal generation of carriers in the depletion region and then the separating of the hole/electron pair by the E field causes a current component. That increases the saturation current.

## Slide 51
Simulated 1D PN junction versus depletion approximation
The depletion approx. is not that good.
These results are for a 1D solution of Poisson’s equation and drift-diffusion transport equations.
Finite difference was used.

## Slide 52: PN Junction (actually NP)
VbcL = floating
Nd = 2e16 and Nd = 1e16
VbcR = 0
Jn = 0 at edges.
Initially carrier densities are bulk
Final
Very slow movement to SS due to very small time steps and almost balanced currents
Φ = 0.7V but it only reaches 0.13V

## Slide 53: PN Junction Force to Equilibrium
Two stage simulation:
  VbcL = Φ (calculated Vbi)
  Vbcl = floating
VbcR = 0
Initially carrier densities are bulk
Final
Quicker movement to equilibrium
2nd stage checks we’re not forcing a solution
n and p equilibrium values at edges

## Slide 54: PN Junction Under Bias
Two stage simulation:
  VbcL = Φ (calculated Vbi)
  VbcL = Φ – 0.3 (fwd bias)
VbcR = 0
Initially carrier densities are bulk
Final
n and p equilibrium values at edges
Net current almost constant across device. (Recombination is present)

## Slide 55: Summary
Semi-classical model of semiconductor
  Two carriers with effective mass
  Drift-diffusion and potential equation
  Essentially a 1st order model of Boltzmann Transport equation
Analytical approaches are very limited
  Use minority carrier injection
  Steady-state
  Simplified geometry and assumptions such as complete depletion approximation.
Numerical approaches are many
  Finite Difference
  Finite Element
  Often very slow due to need for very fine meshing on gradients of doping density.